Item Requirements

○ Article Name: Conductive Adhesive Tape with High Emittance for a Spacecraft

○ Type and Quantity

| Item No. | Item | Q'ty |
| --- | --- | --- |
| 1 | Conductive Adhesive Tape with High Emittance for a Spacecraft | 1 set |

○ Delivery Date: Within 60days after the contraction

○ Requirement:

- Surface Resistivity ≤ 10kΩ/square

- Electric conduction between the tape and the spacecraft are required

- Temperature Range: -60℃ to 65℃

- Low Outgassing

- Total Mass Loss(TML) ≤ 1%

- Collected Volatile Condensed Material(CVCM) ≤ 0.1%

- Optical Properties

- Solar Absorptivity ≤ 0.15

- Emissivity ≥ 0.85

- Adhesion ≥ 15 oz/inch

- Thickness ≤ 255μm

- Weight ≤ 610 g/m^2

- Perforation

- Shelf Life ≥ 12month at normal temperature(10℃ -27℃) after shipment

○ Delivery Item

1. Conductive Adhesive Tape with High Emittance for a Spacecraft