Item Requirements

○ Article Name: Plasma electron source for electric propulsion

○ Type and Quantity

| Item No. | Item | Q'ty |
| --- | --- | --- |
| 1 | Hollow cathode with LaB6 emitter(insert) | 2 |
| 2 | Hollow cathode with BaO impregnated emitter(insert) | 2 |

○ Item Requirements

|  | Item #1 | Item #2 |
| --- | --- | --- |
| Current range | 5 – 20 A(DC) | 0.5 – 3 A(DC) |
| Minimum operation flow rate (Xenon) | ≤ 5 sccm | ≤ 1.0 sccm |
| Minimum self-sustaining power | ≤ 25 W | ≤ 10 W |
| Heater heating current | ≤ 7.0 A(DC) | ≤ 3.5 A(DC) |
| Keeper diameter | ≤ 26 mm | ≤ 20 mm |
| Overall length | ≤ 115 mm | ≤ 80 mm |
| Ignition time | Within 5 min | Within 5 min |
| Operation lifetime | ≥ 1,000 hours | ≥ 1,000 hours |
| Allowable ignition cycles | ≥ 3,000 times | ≥ 3,000 times |

*User manual for each item should be provided.

*User manuals should contain overall dimension (Keeper dimension, mounting holes, tube size, etc), storage condition, electrical circuit diagram, propellant supply pipeline, and operation procedure.